## Technical Specification for Packaging Bags – High Value Agriculture  Crops

### 1️⃣ Product Types

a) Cloth Bags (Reusable)
b) Food Grade Plastic Bags (Primary packaging for fresh Crop)

### 2️⃣ Intended Use

Packaging, storage, handling, and transportation of fresh and processed HVA crops:
Broccoli, Peas, Kidney Beans, Onion (market and cold-chain supply)

## 3️⃣ Cloth Bags – Specifications

| Parameter | Requirement |
| --- | --- |
| Material | 100% Cotton / Jute / Non-woven breathable fabric |
| Food Safety | Must comply with FDA / EU food contact standards |
| Capacity | 1 kg, 2 kg, 3 kg, 5 kg |
| GSM | 120–180 GSM (as per required strength) |
| Weave | Tight plain weave with high tensile strength |
| Stitching | Double-fold edges with lock-stitch; minimum 6 stitches per inch |
| Handle | Soft woven handle for 3 kg and 5 kg sizes |
| Ventilation | Micro ventilation pores for onions & broccoli |
| Colour | Natural/White (non-toxic dyes only if printing required) |
| Printing | Supplier branding, produce label, batch, weight, and date |
| Shelf Life | Minimum 1 year under normal storage |

## 4️⃣ Food Grade Plastic Bags – Specifications

| Parameter | Requirement |
| --- | --- |
| Material | LDPE / LLDPE / HDPE Food-grade certified |
| Thickness | 40–80 microns depending on size |
| Capacity | 1 kg, 2 kg, 3 kg, 5 kg |
| Food Safety | BPA-free, Meets ISO 22000 / FDA / EU 10/2011 Regulations |
| Ventilation (Fresh Crops) | 6–12 perforations (3–6 mm) for Broccoli & Onion |
| Seal Type | Heat-sealed bottom with side gusset for volume expansion |
| Printing | Up to 4-color print for product details and traceability |
| Transparency | Semi-transparent for product visibility |
| Temperature Range | -20°C to +50°C (suitable for cold storage & freezing) |
| Odor & Taste | Odorless, non-reactive, chemical-free |
| Recyclability | Recyclable material preferred |

## 5️⃣ Standard Sizes and Dimensions

| Capacity | Approx. Dimensions (Plastic) | Approx. Dimensions (Cloth) |
| --- | --- | --- |
| 1 kg | 20 cm × 30 cm | 18 cm × 28 cm |
| 2 kg | 25 cm × 35 cm | 22 cm × 33 cm |
| 3 kg | 30 cm × 40 cm | 27 cm × 38 cm |
| 5 kg | 38 cm × 50 cm | 35 cm × 48 cm |

## 6   Quality & Inspection

- Bags shall be free from holes, contamination, and sharp edges

- Random sampling as per ISO 2859-1 AQL standards

- Tensile strength, seam strength, and leakage resistance test for plastic

### ✔️ Deliverables

- Prototype/sample approval before bulk purchasing

- Certificate of food safety compliance with each lot